## Slide 1
ALUMINIUM SCANDIUM NITRIDE
Ferroelectric Memristive device based on the Wurtzite AlScN film(IEEE)
2) A III-V semiconductor based ferroelectric(AIP[Journal of applied physics])
JOURNAL TITLES

## Slide 2
Ferroelectric Memristive device based on the Wurtzite AlScN
PAPER SUMMARY FROM OUR UNDERSTANDING :
The bottle neck faced in the Von Neumann architecture is ,there is a great difference in speeds of memory and speed of the CPU to over come this bottle neck ferroelectric memristive devices are the suitable candidates due to their high switching polarization capabilities in range of nano seconds .The candidate chosen for the ferroelectric thin film material is AlScN which is taken in wurtzite crystal structure and has wide range of supporting factors like .
Remanent Polarization :
It is an important property of ferroelectric material which tells the capability of the material to hold the polarization even when the applied Electric field is removed .
This polarization is Non-Volatile and Reversible and can be achieved in each unit cell for ferroelectric materials.
The best candidate to achieve high remanent polarization is AlScN (Pr >100 uC/cm2 )[Quoted in the paper]
High Breakdown field Strength :
High Coercive Field :
The ferroelectric materials like AlScN has high coercivity which means that the field required to completely make the polarization zero.
Resistance Switching :
Resistance Switching means converting the ferroelectric material’s resistance from high resistance state to low resistance state and this process of conversion from low resistance state to high resistance state is known as SET.
The process of set has a current limitation also known as current compliance which is the maximum current that will be applied
along with high Field to convert the material into a low resistance state which is non volatile and can be reversed back.
The ferroelectric materials have high dielectric constant are and AlScN has a high break down field strength which is useful during polarization switching.

## Slide 3
The current compliance is used for two purposes one is to
i) avoid dielectric break down
ii) Used to modulate the required type of switching
Dielectric Breakdown : If the applied field is so high that the dielectric looses its property of insulation and starts to behave as a conductor is known dielectric breakdown so for in the process of SET there is always a current compliance with low current compliance of 10uA and high current compliance of 1mA the low current compliance tells the minimum current required for the switching of resistance from high to low which can go in repetitive cycles up to high current compliance where stable switching with low polarization losses is achieved and going more than the high current compliance rating makes the device breakdown
The modulation using current compliance for the required switching
Using the amount current applied along with high field during the SET process the type of switching can be chosen in this paper
Unipolar Switching(10 uA current lowest current)
Bipolar Switching(1 mA current)
Unipolar Switching(low current compliance=10 uA) & Bipolar Switching( High current compliance=1 mA ) :
In this paper the device is fabricated for threshold of 1.2 V where switching of resistance happens and a current of 10uA is achieved in this voltage generally there is a loss in polarization so there is no stable switching achieved generally in low current compliance ,gradually increasing the voltage up to 5V to achieve 1 mA which is the high current compliance so a stable switching of resistance from high to low resistance state is achieved
Remanence:
The ability of the device to maintain the low resistance state when subjected with no external field that is 0 V after switching from high resistance to low resistance state i.e.by applying a voltage above the threshold voltage . This property is generally present in ferro electric material but in AlScN it is comparatively higher so becomes a suitable candidate for memristor type devices

## Slide 4
RESET:
The ferroelectric material can be again switched from low resistance state to high resistance state this can be achieved by applying the negative voltage generally there is no current compliance for the reset state.
The capability of the material to hold the polarization charges with less polarization loss after SET and ability of the material to with stand high temperature during the RESET and SET process becomes a necessary quality for the material that becomes the candidate for memristor and the minimum temperature up to which the material can hold with its property is given by curie temperature which is generally higher for AlScN in temperature ranges of greater than (600 °C)
After this temperature the material looses its ferroelectric property and become a paraelectric material which is nothing but the material is a dielectric material where when the applied field to the material when removed the polarization is no longer held by the material any longer

## Slide 5
A III-V semiconductor based ferroelectric
Ferroelectric materials posses spontaneous polarization which is tuneable using field applied to the material generally the ferroelectric materials are used for MEMS and RF switches . The III-V nitride groups have spontaneous polarization along their c axis which occurs due to the separation of group 3 metal an nitrogen atom in same plane therefore two antiparallel polarizations exist causing two phases (Ga-phase and N-phase) in case of GaN .
It is very clear that normal III-Nitrides are not ferroelectric but they are pyroelectric the reason for these nitrides not being ferroelectric is mainly that the critical field required for the polarization to change is so high that the dielectric breakdown happens earlier .
AlScN there by becomes the best candidate as both AlN and ScN exhibit higher piezoelectric polarization due to their higher piezoelectric coefficients.
The amount of scandium content and mechanical stress on the material affect the ferroelectric property of AlScN
The mole fraction ratios in Al(1-x)Sc(x)N where x is the percentage of Scandium in the AlScN where the minimum percentage to have a ferroelectric property of the material and achievable electric field strength before break up is (0.27) which is 27 percent of Sc and 73 percent of Al. the maximum percentage of Scandium that is mentioned in the paper is around 43 percent .
The paper provides relation with percentages of scandium with applied field and corresponding polarizations.
From the hysteresis loop for E field vs polarization it was clear that when increasing the percentage of scandium we found that
The critical field required for to achieve polarization becomes low .but at the same time the retentivity of the polarization also reduces for increased percentage of scandium

## Slide 6
In the Crystal level the U parameter which intern deals with (metal and nitrogen distance)
The decrease observed in polarization trend when Scandium content was increased is due to increase in the u parameter this increase in the crystal parameter causes non polar layered hexagonal structure
The change in lattice parameters is also due to mechanical stress that the AlScN material faces which also causes the polarization to change
The paper also uses Born Effective charge and ionic displacement to find the total spontaneous polarization the Born effective charge is given by ZB it is a tensor Quantity(which is neither Vector nor Scalar) it is 2.5e for AlN.
The ionic displacement is denoted by Δd
Δd =C(1-2U)=1.2A,with c=5A and u=0.38
It was observed that the value of ZB increases with increase in scandium percentages but there is a decrease in ionic displacement as the parameter u increases with increase in metal and nitrogen distance

## Slide 7
THANK YOU